LİNOTEKS NİŞASTA TÜREVLERİ SAN. VE TİC. A.Ş.

Nazmi Akbaci Ticaret Merkezi No.232                   	    	          Tel.: 0212-346 16 84 pbx / Fax:0212-346 16 87

Atatürk Oto Sanayi Sitesi  				          E-mail:  info@linoteks.com

34398 Maslak / İstanbul     			                        www.linoteks.com

LINOSIZE C25

Uses:

Linosize C25 is a vinil  based synthetic polymers and organic polymers developed as sizing materials for a wide range of staple yarns. Especially fine and difficult cotton yarn constructions, polyester-cotton blends, 100% polyester yarn, viscous and similar yarn reaches high weaving efficiency with Linosize C25.

Linosize C25 may be used as the sole ingredient when sizing spun rayon, folded yarns. Linosize C25 should not be used on denim fabric, because of incompatibility of chemicals in the scouring process.

It can be used alone in the recipe without starch for high weaving efficiency or it can be mixed with various kinds of starch.

Characteristics:

Linosize C25 when used alone in the recipe has an excellent adhesion to most spun yarns and produces a tough and flexible film on the yarn. This film is resistant to high humidity and does not soften or stick at high humidity and high room temperature.

At low humidity this film still keeps its flexible character and has minimum warp breackages. Because of the high adhesion to yarn Linosize C25 reduces dusting and loom deposits and also gives a high abrasion resistance.

Application:

Preparation of the size solution. Enter approxmetely two thirds of the required volume of cold water into the mixer and switch on the stirrer. Sprinkle slowly  the Linosize C25  powder into the vortex formed by the stirrer add the softener Linovax K 400.

Stirr 15 minutes in cold water to allow to disperse before starting cooking. Although Linosize C25

is soluable in cold water it is preferable to raise temperatures to 85 – 90 0C for 35 minutes stirring constantly in order to speed up the proces. After cooking wait for minimum 10 minutes before using.

Small amounts of Linosize C25 may enter the discharge shaft at the bottom of the cooking vessel. These particles  will not disperse and will cause problems on the yarn during the following steps.

To avoid this problem and to push these particles out of the pipe small amount of steam should be released from the bottom during the adding of Linosize C25  into the water and during the cold stirring process. The size can be stored hot or cold depending on individual circumstances.  In case of adding starch to the recipe there is no problem cooking it with Linosize C25 .

LİNOTEKS NİŞASTA TÜREVLERİ SAN. VE TİC. A.Ş.

Nazmi Akbaci Ticaret Merkezi No.232                   	    	          Tel.: 0212-346 16 84 pbx / Fax:0212-346 16 87

Atatürk Oto Sanayi Sitesi  				          E-mail:  info@linoteks.com

34398 Maslak / İstanbul     			                        www.linoteks.com

Recommendation of recipe:

Many factors are involved in deciding the optimum size loading. Linoteks technical service will welcome the opportunity to make specific recommendations for individual cases.

Sizing:

Before sizing raise squeeze pressure at zero speed on the sizing machine to 7 KN to prevent too much  Linosize C25 on the yarn at start up. In case long stopps during sizing the yarn on the squeeze roller should be sprinkeled with fresh water to avoid sticking of yarn to each other.

Adjust sizing bath temperature around 850C. The  drying cylinders temperature should not exeed 1200C. Because of high adhesion of Linosize C25 the sizing machine can run at higher speeds with higher squeeze roll presure. In this way the sizing department will produce more and the size consumption per meter yarn will be reduced.

Desizing:

When used as sole ingredient in the size recipe Linosize C25 does not need enzymatic desizing.

Since it is completely water soluable, Linosize C25 can be removed from the yarn with a simple wash in hot alkaline water 850C-950C, pH range between 6,5-8,5 never exceeding 8,5pH.

Lubrication:

Afterwaxing with Linowax D 40 is strongly recommended to improve weavability. The liquid vax should be applied at the rate of 0,3%-0,5% on weight of yarn from an afterwaxing roller.

Size recovery:

The high water-solubility of the Linosize products makes them suitable for recovery from woven fabric by a pad-squeeze technique. By using the minimum amount of water in the early stages of desizing a sufficiently concentrated solution can be obtained to make it suitable for re-use after addition of fresh size.

When ultrafiltration equipment is available, Linosize products can be recovered successfully by this method. However in such a situation it is preferable to use a size in its pure form and not in admixture with other sizes. Linosize C25  is recommended for this purpose.

Linosize C25  has the adventages of being very resistant to high humidity in the weaving shed and, being non-ionic, does not pick up salts during the recycling process. For further information on this please contact our Technical Department.

LİNOTEKS NİŞASTA TÜREVLERİ SAN. VE TİC. A.Ş.

Nazmi Akbaci Ticaret Merkezi No.232                   	    	          Tel.: 0212-346 16 84 pbx / Fax:0212-346 16 87

Atatürk Oto Sanayi Sitesi  				          E-mail:  info@linoteks.com

34398 Maslak / İstanbul     			                        www.linoteks.com

Storage life:

12 months when kept dry. It is not effected by freezing temperature

Packaging:

Linosize C25  is sold in 25 kg polyproplen bags on one ton shrinked pallets