LİNOTEKS  NİŞASTA TÜREVLERİ   SAN. ve TİC. A.Ş.

Nazmi Akbaci Ticaret Merkezi No.:232                       		    Tel.: +90-212-286 24 00 pbx / Fax:.: +90-212-286 24 03

Atatürk Oto Sanayi Sitesi  80670 Maslak / İstanbul     		     E-mail:  linoteks@superonline.com

LİNOSİZE TOK

Uses:

Linosize TOK is a vinil  based synthetic polymers developed as sizing materials for a wide range of staple yarns. Especially fine and difficult cotton yarn constructions, polyester-cotton blends, 100% polyester yarn, viscous and similar yarn reaches high weaving efficiency with Linosize TOK.

Linosize TOK may be used as the sole ingredient when sizing spun rayon, folded yarns, and for yarn used in certain special fabrics, such as towels, velvets and surgical dressing mull.

Linosize TOK should not be used on denim fabric, because of incompatibility of chemicals in the scouring process.

Linosize TOK does not contain starch. It can be used alone in the recipe without starch for high weaving efficiency or it can be mixed with various kinds of starch.

Characteristics:

Linosize TOK when used alone in the recipe has an excellent adhesion to most spun yarns and produces a tough and flexible film on the yarn. This film is resistant to high humidity and does not soften or stick at high humidity and high room temperature.

At low humidity this film still keeps its flexible character and has minimum warp breackages. Because of the high adhesion to yarn Linosize TOK reduces dusting and loom deposits and also gives a high abrasion resistance.

Application:

Preparation of the size solution. Enter approxmetely two thirds of the required volume of cold water into the mixer and switch on the stirrer. Sprinkle the Linosize TOK  powder into the vortex formed by the stirrer add the softener Linovax K 400.

Stirr 15 minutes in cold water to allow to disperse before starting cooking. Although Linosize TOK

is soluable in cold water it is preferable to raise temperatures to 85 – 90 0C for 35 minutes stirring constantly in order to speed up the proces. After cooking wait for minimum 10 minutes before using.

Small amounts of Linosize TOK may enter the discharge shaft at the bottom of the cooking vessel. These particles  will not disperse and will cause problems on the yarn during the following steps.

To avoid this problem and to push these particles out of the pipe small amount of steam should be released from the bottom during the adding of Linosize TOK  into the water and during the cold stirring process. The size can be stored hot or cold (if no starch is present) depending on individual circumstances.  In case of adding starch to the recipe there is no problem cooking it with Linosize TOK .

Recommendation of recipe:

Many factors are involved in deciding the optimum size loading. Linoteks technical service will welcome the opportunity to make specific recommendations for individual cases.

LİNOTEKS  NİŞASTA TÜREVLERİ   SAN. ve TİC. A.Ş.

Nazmi Akbaci Ticaret Merkezi No.:232                       		    Tel.: +90-212-286 24 00 pbx / Fax:.: +90-212-286 24 03

Atatürk Oto Sanayi Sitesi  80670 Maslak / İstanbul     		     E-mail:  linoteks@superonline.com

Sizing:

Before sizing raise squeeze pressure at zero speed on the sizing machine to 7 KN to prevent too much  Linosize TOK on the yarn at start up. In case long stopps during sizing the yarn on the squeeze roller should be sprinkeled with fresh water to avoid sticking of yarn to each other.

Adjust sizing bath temperature around 850C. The  drying cylinders temperature should not exeed 1200C. Because of high adhesion of Linosize TOK the sizing machine can run at higher speeds with higher squeeze roll presure. In this way the sizing department will produce more and the size consumption per meter yarn will be reduced.

Desizing:

When used as sole ingredient in the size recipe Linosize TOK does not need enzymatic desizing.

Since it is completely water soluable, Linosize TOK can be removed from the yarn with a simple wash in hot alkaline water 850C-950C, pH range between 6,5-8,5 never exceeding 8,5pH.

Lubrication:

Afterwaxing with Linowax D 40 is strongly recommended to improve weavability. The liquid vax should be applied at the rate of 0,3%-0,5% on weight of yarn from an afterwaxing roller.

Size recovery:

The high water-solubility of the Linosize products makes them suitable for recovery from woven fabric by a pad-squeeze technique. By using the minimum amount of water in the early stages of desizing a sufficiently concentrated solution can be obtained to make it suitable for re-use after addition of fresh size.

When ultrafiltration equipment is available, Linosize products can be recovered successfully by this method. However in such a situation it is preferable to use a size in its pure form and not in admixture with other sizes, especially starches. Linosize TOK  is recommended for this purpose.

Linosize TOK  has the adventages of being very resistant to high humidity in the weaving shed and, being non-ionic, does not pick up salts during the recycling process. For further information on this please contact our Technical Department.

Storage life:		12 months when kept dry.

Packaging:		Linosize TOK  is sold in 25 kg polyproplen bags on one ton shrinked pallets

All product names in capital letters are either registered or pending trademarks and property of Linoteks Nişasta Türevleri Sanayi ve Ticaret A.Ş.

IMPORTANT: The following supersedes Buyer’s documents. SELLER MAKES NO PRESENTATION OR WARRANTY, EXPRESS OR IMPLIED, INCLUDING OF MERCHANTABILITY OR FITNESS FOR A PARTICULAR PURPOSE. No statements herein are to be construed as inducements to infringe any relevant patent. Under no circumstances shall Seller be liable for incidental, consequential or indirect damages for alleged negligence, breach of warranty, strict liability, tort or contract arising in connection with the producesr(s). Buyer’s sole remedy and Seller’s sole liability for any claims shall be Buyer’spurchase price. Data and results are based on controlled or lab work and must be confirmed by Buyer by testing for its intended conditions of use. The product(s) has not been tested for, and is therefore not recommended for, uses for which prolonged contact with mucous membranes, abraded skin, or blood is intended; or for uses for which implantation within the human body is intednded.

Please note that products may differ from country to country. If you have any qyeries, kindly contact your local Linoteks Nişasta Türevleri Sanayi ve Ticaret A.Ş representative.